- CUTTING WITH BROCO

Virtually all metals and other materials can be cut, burned, pierced or melted with the Broco Underwater Ultrathermic system.

- Broco cuts all, including the cost of cutting.

- Cutting an old H-beam? Forget about pre-cleaning the area to be cut. Broco cuts right through the fouling. Strike an arc on a striker plate and go.

- Notching a rock for a lift cable? Broco's high tip temperature will melt granite underwater.

- Removing wire rope or line from a wheel? The Broco Underwater Ultrathermic system will cut it whether steel, nylon, hemp or sisal. Just be careful not to contact the shaft.

- Trimming a propeller blade? Drilling or sawing is painfully slow. Melt through phosphor-bronze or other similar alloys on the biggest wheel with your Broco system.

- Removing a composite piling? You don't need two different tools to cut two different materials.

- Trimming a cement-covered submarine pipeline? Your Broco system will cut or melt through the concrete, wire mesh, wrap, mastic or pipe.

- The Broco Underwater Ultrathermic cutting system does it all.

WARNINGS AND SAFETY PRECAUTIONS

WARNINGS:

All users and their supervisory personnel must read and be thoroughly familiar with these operating instructions prior to using this equipment.

Never modify this equipment in any manner or use it in any way not specified in these instructions.

Always adhere to ANSI/ASC Z49.1-88 "Safety in Welding and Cutting" standards, or similar locally prevailing standards when using this equipment.

Always follow industry accepted safe diving practices as found in the Association of Diving Contractors "Consensus Standards for Commercial Diving."

Always use surface supplied breathing air and hard-wire communications. Never conduct underwater cutting or welding while using self-contained breathing apparatus (SCUBA).

Never conduct underwater cutting or welding operations without a topside tender to monitor the diving operation and a standby diver for emergency response.

Never use life support equipment that has been altered or modified from the manufacturer's original specifications.

Never use any equipment that is unsafe or appears to be unsafe. Always replace damaged or worn components to reduce the risk of injury.

Never use a "burning bar" for underwater cutting operations. A burning bar is considered to be any underwater cutting electrode operating with oxygen as a fuel source whose diameter is greater than 3/8" and length is longer than 36".

Always be aware of material that may fall and position yourself and your life support equipment accordingly.

SAFETY PRECAUTIONS:

WARNING: Failure to heed these safety precautions may result in severe property damage, bodily injury or death.

Protect yourself and others. Explosive gas mixtures may be generated. Arc rays can injure eyes and exposed skin. Electric shock can kill. Oxygen mixed with oil or grease reacts explosively.

Always keep the ignited tip of the rod away from any part of the operator's body, hoses, cables and compressed gas cylinders.

Always provide for adequate ventilation (venting) of the area behind and above the cut to provide for the escape of gases generated during cutting. Underwater cutting operations can lead to the build up of potentially hazardous explosive gas mixtures that may be ignited by a spark from the ignited cutting rod.

Always know what is behind the material being cut.

Always purge closed chambers with inert gas (such as argon or nitrogen) prior to initiating underwater cutting or welding operations.

Always keep oil and grease away from oxygen cylinders, valves, regulators, hoses and fittings.

Never use compressed air, oil, solvents or other material to clean the oxygen system. The oxygen system could become contaminated and cause internal burning in the torch or hose. A qualified and knowledgeable technician must perform all service on oxygen delivery parts.

Never energize a cutting rod unless to immediately initiate underwater cutting. Explosive gases can accumulate within an energized underwater cutting rod. The cutting rod must be purged with oxygen by squeezing and holding the oxygen lever for at least four seconds with the rod in cutting position prior to energizing the cutting rod and initiating the arc.

Never use alternating current (AC) for any underwater operation.

Always ensure only direct current (DC) from a known power source goes into the water.

Always have electrical power to the torch routed through a safety knife switch that must be located within reach of the topside tender.

Never touch live electrical parts. Always ensure the electrical power is off when changing cutting or welding electrodes to reduce the risk of shock or electrically caused damage to the diver's life support equipment.

Always wear adequate protective clothing. The diver must be equipped with proper diving dress in good condition.

Never use this equipment without proper eye protection. Always use an approved welding lens with a shade appropriate for the conditions of the water.

Always wear rubber electrical insulating gloves when using this equipment.

See: American National Standard Z49.1-88 "Safety in

Welding and Cutting" published by the American Welding

Society, 550 N.W. LeJeune Rd., Miami, FL 33126,

Tel. 305.443.9353

"Consensus Standards for Commercial Diving", published by the Association of Diving Contractors, 3910 FM, 1960 West, Suite 230, Houston, TX 77068, Tel. 281.893.8388.

OSHA Safety and Health Standards "29 CFR 1910" available from the U.S. Department of Labor, Washington, D.C. 20210, Tel. 202.693.1999.

THE BROCO SYSTEM

Made for divers by diversÔ, the Broco system maximizes diver performance, safety and ease of use. The system consists of a series of components, designed to work together, which go from the oxygen cylinder to the work-piece.

The patented Broco Underwater Ultrathermic Cutting Rod.

- 18" or 36" long, 3/8" or 1/4" diameters.

- 2" safety recess at the torch end.

- Seven interior alloy core wires provide a burning temperature of approximately 10,000° F (5,500° C) at the tip.

- Copper coated for better conductivity and corrosion resistance.

- Trademark wrapped insulation won't chip or flake off, even when the rod is bent.

- Cutting rod continues to burn as long as oxygen is flowing, even with power off.

The Broco BR-22 Oxy-Arc Cutting torch.

- Designed for maximum oxygen flow, use with Broco Underwater Ultrathermic Cutting Rods to achieve performance cutting at any depth.

- Offset handle design decreases forearm fatigue.

- Acme threaded torch head and collet nut won't foul from grit, sand or slag.

- All-brass metal parts reduce electrolysis for long service life.

- Oxygen valve electrically isolated from torch head through the use of a flexible rubber coupler.

- Two-piece body and threaded internal connections permit rapid disassembly and field service.

- International orange for maximum visibility.

The Broco HVR-4401 Oxygen regulator.

- High oxygen flow: 4400cu.ft. /hour, over 70c.f.m.

- Two-stage design, first stage reduces cylinder pressure by 90%.

- Large second stage diaphragm for precise adjustment, accurate and constant delivery at uniform pressure.

- Vented and equipped with internal pressure relief valve between stages.

- Inlet filter to keep out foreign matter.

- Underwriter's Laboratory approved.

OPERATING INSTRUCTIONS

Equipment Required.

- Broco BR-22 cutting torch, preferred because it is designed for diver comfort, maximum oxygen flow, and ease of operation and maintenance.

- Broco Underwater Ultrathermic Cutting Rods.

- Broco HVR-4401 high volume two-stage oxygen regulator.

- Single pole single throw or double pole single throw safety knife switch. (Rated 400 amps DC, unfused.)

- C-type grounding clamp. (Appropriate for underwater use.)

- 150-200 amp 100% duty cycle DC welding power source or 12v or 24v battery.

- Size 1/0 (minimum) welding cables for torch power and ground leads.

- Oxygen supply. (Gas only, 99.5% purity minimum.)

- 3/8" inside diameter oxygen supply hose. (Regulator to torch. Taped to torch power cable at 2' intervals.)

Rigging for Underwater Cutting Operations. (Setup)

Warning: Never use alternating current (AC) for underwater cutting operations. AC in the water can kill or seriously injure the diver and others.

Never operate the torch without the flash arrestor and flash arrestor screen in place.

Always keep oil and grease away from oxygen cylinders, valves, regulators, hoses and fittings. Oxygen mixed with oil or grease reacts explosively.

Always use a Broco Underwater cutting torch. Never use a torch designed for topside use for underwater cutting. Shock to the diver may occur.

Always use Broco Underwater Cutting Rods with the Broco torch. Never use a cutting rod not intended for underwater use. Shock to the diver may occur.

Always use only Broco replacement parts in the Broco underwater torch.

Always ensure the safety knife switch is in the open position before starting the welding power source.

Never lower the torch into the water or raise the torch from the diver with a cutting rod in place.

1. Before beginning, inspect components to ensure that:

A.	Hose and cables are in good condition with no visible cuts, cracking or splitting. Cable lug connectors should be securely attached and without visible excessive corrosion.

B.	All electrical connections must be made watertight by carefully taping with UL approved electrical insulating tape. Tape should extend at least 4" up the cable on both sides of the connection.

- Cutting torch is in good condition with no visible gaps in the seam between the handle halves. Torch should be inspected to make sure flash arrestor, clean flash arrestor screen, neoprene compression washer, collet washer and appropriate size collet are in good condition and in place.

To replace the collet:

- Remove the collet nut and collet from the torch.

- Make sure the neoprene collet washer is in place.

- Insert the desired collet and replace the collet nut.

D.	Welding power source is DC output.

E.	Diver is equipped with proper diving dress and life support equipment in good condition. Rubber "linesman" gloves must be worn in addition to other gloves the diver may have.

F.	Appropriate eye protection is attached to the diver's faceplate. Use an approved welding lens. A minimum #4 shade is usually suggested for muddy water, #6 shade for average conditions and #8 shade or above for clear water, however the diver must use his best judgment as experience and conditions dictate.

Warning: Never stand directly in front of or directly behind the oxygen regulator while opening the oxygen cylinder valve to reduce the risk of injury in the unlikely event of regulator failure.

NOTE:	Set the welding power source to 150 amps delivered to the torch; and the oxygen regulator delivery pressure to 90 psig over ambient pressure.

- Attach the oxygen regulator to the oxygen supply and the oxygen supply hose to the regulator outlet. Make sure the supply valve, regulator, hose and torch are clean and free of any grease, oil or particles. Purge the regulator and hose with oxygen to clear any obstructions.

- Attach the torch to the oxygen supply hose.

- Set the regulator delivery pressure to 90 psig over the ambient bottom pressure or other pressure which may be required due to depth or nature of operation. Regulator delivery pressure must be increased with increased working depth. (See Table- "Setting Oxygen Delivery Pressure for Depth.")

- Purge the torch. Check fittings, connections and the torch for leaks using soap suds.

- Attach the safety knife switch to the torch power lead. Attach the other end of the torch power lead to the torch cable. Attach a cable from the welding power source negative terminal to the safety knife switch. Ensure the safety knife switch is positioned within reach of the tender. The safety knife switch is activated only upon command from the diver. Wrap all cable-to-cable connections with rubber strips and electrical tape.

- Attach the ground cable to the welding power source positive terminal. Attach the other end of the ground cable to the ground clamp.

- With the safety knife switch in the open position, start the welding power source and set output for 150 amps maximum at the rod tip. (See Table "Setting Amperage for Cable Length and Size.")

- Check polarity by immersing the rod tip and ground clamp in a bucket of salt water approximately 2" apart. Energize the rod by closing the safety knife switch. A stream of bubbles should rise from the rod tip. If not, reverse the polarity and retest.

- Check amperage using a clamp-on or in-line gauge. Do not rely on dial indicators on the welding power source.

Once the diver is in the water: Warning: Never turn your back to the ground connection. Serious shock hazard to the diver and electrolytic damage to the diver's helmet and life support equipment can result if the diver's body comes between the cutting rod and the ground. Never touch the cutting rod to any metal on the diver's dress or equipment.

- Secure the ground clamp to the workpiece as close to the area to be cut as possible. Ensure that the ground is away from the diver as he proceeds to cut.

- Check that oxygen delivery pressure is correctly set by squeezing the torch lever to release a stream of oxygen. A 6" jet of oxygen should issue from the cutting rod tip.

Starting to Cut. Warning: Never use a damaged Ultrathermic cutting rod. Always insert the correct end of the rod into the torch. Never energize the rod unless it is in position to initiate cutting and the diver has maintained a flow of oxygen for at least four seconds to purge the rod of explosive gases. Never let the Ultrathermic cutting rod bum down into the torch.

Always release the oxygen lever to extinguish the torch while there is at least 2" of rod remaining to avoid damage to the torch. Always use Broco Underwater products with the Broco Underwater BR-22 cutting torch. Broco Underwater Ultrathermic cutting rods are specially designed for use with the Broco Underwater BR-22 cutting torch. Never use rods of other manufacture as hazardous backflashes or internal burning may result.

NOTE:	Broco Underwater Ultrathermic Cutting Rods will continue to burn as long as the oxygen flow is maintained, even with the power off. The oxygen lever must be released to extinguish the cutting rod.

- Loosen the torch collet nut 1/2 turn.

- Insert the end of the Broco Underwater Ultrathermic cutting rod that has the recessed internal wires into the collet opening until it bottoms on the collet washer.

- Tighten the collet nut to lock the rod in place.

- Check for oxygen leaks at the collet nut and around the collet by squeezing the oxygen lever. If a leak exists: make sure the rod is firmly seated on the collet washer; inspect the rod for damage; inspect the collet washer for damage and replace if necessary.

- Place the tip of the rod against the work at the point where the cut is to be initiated and squeeze the oxygen lever for four seconds to purge the rod and torch.

- With the oxygen still flowing call for the current to be switched on. The tender will close the safety knife switch.

- Draw the tip of the cutting rod across the work to strike the arc.

- Once the arc is struck and the rod ignited, pull (drag) the cutting rod along the line to be cut. The angle of the rod to the work should be between 30 and 90 degrees, depending on the metal thickness.

- Maintain pressure to keep the rod against the work. Keep the tip of the rod in the puddle at all times. Move slowly at first, making sure full penetration is achieved. As cutting speed is increased, back spray and increased cutting noise will indicate insufficient penetration.

NOTE:	Do not try to hold an "arc". Keep the tip of the burning rod in direct contact with the target material at all times.

Hold the rod "like a pool cue" with your free hand approximately 4" from the rod tip for a more stable cut. Keep moving the hand back as the rod consumes.

- When the rod has burned to within approximately 3" of the torch collet nut call for the current to be switched off.

- Lift the rod from the work and release the oxygen lever to extinguish the cutting rod.

- After the tender has confirmed the current is off, loosen the collet nut 1/2 turn and squeeze the oxygen lever to blow the rod stub from the torch.

- Insert a new cutting rod and repeat the process until the cut is complete.

NOTE:	When cutting or melting non-conductive materials such as concrete, rock, coral, mastic, rope or marine growth, a striker plate (consisting of a steel or copper plate connected to the ground cable) is necessary to initiate the arc and light the rod. Once the rod is ignited, maintain the oxygen flow and bring the rod into contact with the target material.

45°-90°

PULL TO CUT

KEEP THE ROD TIP AGAINST THE WORK.

TECHNIQUES

NOTE:	Continuous power is recommended for cutting with the 1/4" diameter Broco Underwater Ultrathermic Cutting Rod, otherwise it is difficult to maintain ignition.

Cutting Steel.

The 1/4" diameter Broco Underwater Ultrathermic Cutting Rod may be used for cutting steel up to 1/2" in thickness for maximum cutting economy. The 1/4" rod leaves a narrow kerf and is preferable for fine cutting.

In bad visibility or for thicker steels, the 3/8" diameter cutting rod will give better production. For materials 1/2" thick or thicker, the 3/8" rod is preferable. For metal several inches thick, employ saw and wedge cutting (analogous to chopping wood) to achieve full penetration.

"Rule of Thumb" estimates:

| ROD DIA. | PLATE THICKNESS | RANGE OF CUT |
| --- | --- | --- |
| 1/4” | 1/4” | 20”-25” |
| 1/4” | 1/2” | 10”-15” |
| 3/8” | 1/2” | 12”-20” |
| 3/8” | 1” | 9”-14” |
| 3/8” | 1½” | 8”-12” |

NOTE:	The U.S. Navy Underwater Cutting and Welding Manual, NAVSEA 0929-LP-000-8010, gives estimates for the 3/8" Broco Ultrathermic Cutting Rod at the high end of these ranges.

Cutting Cast Iron, Stainless Steel and Non-Ferrous Metals.

The Broco Underwater Ultrathermic Cutting Rod will melt all of these materials. Make sure that the tip is firmly buried in the work. Saw and wedge cutting may be necessary. Maximum cutting efficiency may be achieved by burning a series of holes through the piece prior to cutting across it.

Cutting Thick Non-Ferrous Metals.

NOTE:	Increase oxygen delivery pressure to 110 psig over ambient pressure for metal over 3" in thickness.

Create a puddle and dip the rod tip slightly below the surface of the molten metal. From time to time push the cutting rod deeper into the metal to wash it out and blow the slag away.

Cutting (Melting) Concrete and Rock.

NOTE:	Always use the 3/8" diameter Broco Underwater Ultrathermic Cutting Rod when cutting concrete or rock.

Light the rod by striking the tip against a copper or steel plate attached to the ground cable. Keep the oxygen lever depressed and raise the rod from the plate to the workpiece. Press the rod tip into the material to create a molten pool. While melting through the material, periodically move the rod in and out and around to vent the cut and allow the oxygen to blow the molten material away.

Cutting Rope and Wood.

Light the rod by striking the tip against a copper or steel plate attached to the ground cable. Keep the oxygen lever depressed and raise the rod from the plate to the workpiece. Apply firm pressure to the tip to keep the maximum heat in direct contact with the material to be cut. In ship work, the rod may be angled or bent up to 90 degrees to prevent damage to the hull, shaft or stern tube. On wire rope the 1/4" diameter rod may be used for finer cut control. When using the 1/4” rod, continuous metal to metal contact is necessary to maintain rod ignition.

Using 3/8" Broco Underwater Ultrathermic Cutting Rods With a Battery.

Caution: Do not use the vessel's primary battery as a power source for rod ignition. Damage or wear to the battery could render the vessel inoperable.

NOTE:	Use of a battery power source is not recommended for cutting at depths below 60 fsw.

A vehicle or boat battery (12v or 24v DC) may replace a welding machine as the ignition power source. The use of a safety knife switch is recommended, although jumper cables may be used as the make/break connection. To preserve battery life, the tender must disconnect the battery immediately on the diver's command once the rod is ignited.

Using 3/8" Broco Underwater Ultrathermic Cutting Rods Without Electrical Ignition.

Warning: Never operate the torch in an explosive or flammable environment.

To make a cut in very shallow water, the rod may be ignited on the surface and submerged to do the work. If an electrical ignition source is not available, the rod can be ignited with a gas torch, or a flame source and piece of wood.

If using wood and a flame source:

- Ensure there are no combustibles nearby or immediately downwind.

- Place a piece of wood at least 2" thick on a non-flammable surface.

- Position a lit match (or other flame source) on the wood.

- Use a very low flow of oxygen from the rod to flame the wood.

- Press the tip of the rod into the charred wood to create a hot pocket, increase the oxygen flow slightly and heat the rod tip to incandescence.

- Hold the rod in position. Ignition will occur in 3-7 seconds.

NOTE:	This technique requires a delicate touch on the torch valve lever to keep excess oxygen from cooling the rod tip or blowing the flame away from it.

Surface Practice.

Warning: Always remove the tape insulation from the cutting rod before burning at the surface. Fumes from burning tape can be harmful to your health. Always keep your head away from the fume plume. Always wear adequate protective clothing, welder's gloves, and face and appropriate eye protection.

Cutting with Broco Underwater Ultrathermic Cutting Rods requires practice. A diver with surface arc welding or cutting qualifications will get excellent results underwater in a short time.

Burning at least three or four rods on the surface before attempting to cut underwater is essential to gaining maximum proficiency with the Broco Underwater Ultrathermic Cutting System.

Do not try to "maintain an arc." Instead practice metal to metal contact, keeping the rod tip in the molten puddle, and adjusting travel speed to ensure complete penetration.

MAINTENANCE

Warning: Never used compressed air to clean or dry any part of the torch, regulator or cutting rods. Compressed air may be contaminated with oil. Always use oxygen as a compressed gas when working on any oxygen components.

NOTE:	Always place a protective cap or piece of tape over the open end(s) of the oxygen hose to prevent dirt or foreign objects from entering during storage.

A medium size standard screwdriver is required for removing the flash arrestor and flash arrestor screen.

Always replace worn or damaged parts with Broco factory replacement parts.

Maintaining the torch.

- After each use remove the collet nut, compression washer, collet, collet washer, flash arrestor and flash arrestor screen and inspect for wear, corrosion damage and foreign matter. Clean or replace as necessary.

- Rinse the torch in fresh water to clean the exterior and flush the interior.

- Purge with oxygen.

- Reassemble the torch with cleaned or new parts.

Maintaining the Oxygen regulator.

Warning: Only qualified and knowledgeable regulator repair technicians should disassemble, reassemble or otherwise repair the oxygen regulator.

- Before each use, prior to connecting the oxygen hose, purge the regulator with oxygen from a high-pressure supply to blow out any foreign matter.

- After each use, the regulator should be wiped with a clean oil-free cloth and stored in a clean dry place.

Maintaining the cutting rods.

- If rods are taken into salt water, rinse with fresh water and allow to dry.

- Store in clean dry place.

TROUBLESHOOTING

Broco Underwater Ultrathermic Cutting Rods are different from steel tubular cutting rods in that Broco Underwater Ultrathermic Cutting Rods require higher oxygen flow and lower amperage. Additionally Broco Underwater Ultrathermic Cutting Rods require direct contact with the work, not maintenance of an arc. Most operational problems stem from operators using steel tubular cutting rods' setup and cutting techniques.

Oxygen supply problems:

- Efficient cutting with Broco Underwater Ultrathermic Cutting Rods relies on high volume unobstructed oxygen flow. With inadequate oxygen flow, the rod can burn without significantly affecting the work.

Symptoms include: the rod burning longer than 60 seconds of continuous use; cuts of less than 12" in 1/2" thick steel plate; and an oxygen jet of less than 6" length underwater.

Solutions:

- Ensure that a high volume two stage oxygen regulator and 3/8" oxygen hose are being used.

- Ensure that the hose is not kinked, pinched or obstructed.

- Ensure that the oxygen cylinder valve (valves if using a manifold system) are fully opened.

- The Broco Underwater Ultrathermic Cutting Rod requires oxygen of at least 99.5% purity to sustain ignition without power. Cutting with continuous power, a reduction in the purity of the oxygen by 1% can decrease cutting efficiency by 25%.

If the rods continuously extinguish underwater, or burn erratically, the problem is probably poor quality oxygen.

Solution:

- Obtain a source of oxygen from a different, unrelated supplier.

NOTE:	Since a gas supplier will usually have all his oxygen coming from one manufacturer, changing cylinders for one filled at the same place or time will not solve oxygen purity problems, Using oxygen of other manufacturer will either solve or rule out an oxygen purity problem.

Power source problems:

- If the rods consume too quickly, it is likely the welding power source is delivering greater than 150 amps.

Solution:

- Use an in-line or clamp type ammeter to verify current output. Adjust as necessary.

Broco, Inc.

8690 Red Oak St.

Rancho Cucamonga, CA 91730 USA

Ph: (909) 483-3222 (800) 845-7259  Fax: (909) 483-3233

e-mail Broco@Worldnet.att.net

www.brocoinc.com

© Copyright 2000 by Broco, Inc., all rights reserved. Any reproduction in whole or in part without the express written permission of Broco, Inc. is expressly prohibited.

Table #1

Setting Oxygen Delivery Pressure for Depth

Depth	                                           Pressure Gauge Setting

ft	m	psig	kpa
	33	10	108	7.4
	40	12	112	7.6
	50	15	117	8.0
	60	18	123	8.4
	70	21	128	8.7
	80	24	134	9.1
	90	27	139	9.5
	100	30	145	9.9
	110	34	150	10.2
	120	37	155	10.5
	130	44	161	11.0
	140	43	166	11.3
	150	46	172	11.7
	160	49	177	12.0
	170	52	183	12.5
	180	55	!88	12.8
	190	58	194	13.2
	200	61	199	13.5
	210	64	204	13.9
	220	67	210	14.3
	230	70	215	14.6
	240	73	221	15.0
	250	76	226	15.4
	260	79	232	15.8
	270	82	237	16.1
	280	85	243	16.5
	290	88	248	16.9
	300	91	254	17.3

310	94	259        17.6

320	98	264	18.0
	330	101	270	18.4
	340	104	275	18.7
	350	107	281	19.1

When depths exceed 350 feet, calculate your gauge pressure as follows:

For every 10' of hose required, add 1 psig to the 90 psig necessary at the tip. This compensates for frictional line losses. Additionally, add 0.445 psig for every foot of working depth.

Table #2

Setting Amperage for Cable Length and Size*

Length of	Amperage setting
Power Cable	for Cable Size

(supply to work
distance)

ft	m	# 1/0	#2/0	#3/0
	150	46	155	152	150
	200	61	157	154	152
	250	76	159	156	154
	300	91	161	158	156
	350	107	163	160	158
	400	122	165	162	160
	450	137	167	164	162
	500	152	169	166	164

*The increases in amperage compensate for resistance losses.

For greater lead lengths, add 2 amperes per fifty feet to settings.

Calculating Pressure and Amperage Settings

Example: A working dive to 560 ft.

Required: 150 amperes at the rod tip plus 90 psig over bottom.

Given: 650' of hose, and #2/0 cable.

Pressure calculations:
	560 ft x 0.445 =249.2 psig
	plus
	650 ft of hose x I psig
	for each 10' of hose = 65.0 psig

plus
	base requirement = 90.0 psig
	Total = 404.2 psig

Set gauge at 404.2 psig to deliver 90 psig at the rod tip at 560' depth with 650' hose.

Amperage calculations:

For 650' of #2/0 cable, start with 166 amperes for 500', and add 6 amperes for 3 additional 50' sections = 172.0 amps.

NOTES