# 4	NDT TECHNIQUES AND PROCEDURES

This section provides detailed procedural requirements for NDT (ultra sonic wall thickness and cathodic potential measurements and M.P.I.) as will be required during the course of routine inspection work.

In those instances where a more specialised N.D.T. technique, for example radiography, ultrasonic flaw detection or eddy current inspection is required, a specific procedure shall be formulated for each individual job. Hence these techniques are not covered here.

  - ULTRASONIC WALL THICKNESS INSPECTION

    - EQUIPMENT REQUIREMENTS

- Normally wall thickness measurements shall be carried out using a digital display ultrasonic thickness gauge such as the Baugh & Weedon Seaprobe P-200 or the Wells-Krautkramer DMU.

- When there is a requirement for the measurement of wall thickness of less than 5mm, testing shall be carried out using an A scan unit (incorporating a CRT display) such as the Wells-Krautkramer USK7 or similar, in conjunction with a Cygnus I probe ( range 0.75mm to 99mm) or similar. Such  A-Scan units shall only be used by a suitably qualified operator.

    - INSTRUMENT CALIBRATION

- It is absolutely essential that the ultrasonic thickness gauge in use is reading accurately at all times. For this reason the calibration of the instrument must be checked against a suitable step-wedge on deck prior  to the dive, at depth prior to the taking of the first reading and at depth immediately after taking the last reading.

- The calibration check on deck prior to diving will, in most cases, prevent wasted diving time due to malfunction of equipment.

- For normal operations a precision-machined step wedge comprising 5mm, 10mm, 20mm and 30mm thick steps shall be used for calibration checks. Calibration using a test piece of one thickness is not acceptable.

All calibration information is to be recorded in ink in table form using a format similar to that shown below:

|  |  | Calibration | Time | Wall Thickness (mm) |  |  |  | Potential (-v) |  | Initials |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 5.0 | 10.0 | 20.0 | 30.0 | Zn | Mg |  |
| Date | Meter (s) | Pre-Dive |  |  |  |  |  |  |  |  |
| Dive No. | Serial No. | Pre-Inspection |  |  |  |  |  |  |  |  |
|  |  | Post-Inspection |  |  |  |  |  |  |  |  |

Note: This form also incorporates the calibration information for cathodic potential measurements.

- Both the Seaprobe P-200 and the WK-DMU meter have a factory rated accuracy of +/- 0.2mm under standard test conditions. Should the calibration readings obtained differ from the specified thickness of the test piece by +/- 0.2mm or more the meter is to be considered non-operational and is to be repaired or replaced.

- If the pre-dive and pre-inspection calibration readings obtained were acceptable but the post-inspection ones are not, all readings taken during the dive are to be retaken using another meter.

- It is often mistakenly stated that the ultrasonic meters designed for underwater use require a 30-minute settling down period prior to use and hence should be immersed in a bucket of water before a dive. This is incorrect; such units require no settling down period and are ready for use immediately they are submerged.

    - TESTING REQUIREMENTS

- Prior to diving ensure that the meter in use has been fully charged and has had its calibration checked.

- The contractor shall perform all charging or changing of batteries in a timely manner so as to ensure that the inspection program is not interrupted.

- In the absence of any protective coating or in the presence of poorly bonded, non-uniform coating the measurement location shall be cleaned to bare, shiny metal finish before any readings are taken.

- In the presence of a well-bonded uniform coating the readings may be taken without removal of the coating. Such readings that include the coating thickness shall be clearly identified in the final report.

- In areas where loss of wall thickness of 1.5mm or more is present due to pitting, pit depths shall be measured using an appropriate pit gauge.

  - CATHODIC PROTECTION MEASUREMENTS

    - EQUIPMENT REQUIREMENTS

- Normally cathodic potential readings shall be taken relative to a silver / silver chloride reference half cell using a diver hand held digital meter such as the Roxby Mk. V Bathycorrometer or the Morgan Berkeley Rust Reader.

- Where specifically approved by the client, in writing, a proximity probe, either hand-held or ROV mounted may be used. In these cases the probe shall be referenced to a silver / silver chloride half-cell.

INSTRUMENT CALIBRATION

It is essential to ensure that the Bathycorrometer in use is reading accurately at all times. For this reason the calibration of the instrument must be checked against zinc (Zn) and magnesium (Mg) test blocks on deck prior to each dive, at depth immediately before taking the first reading and at depth immediately after taking the last reading.

All calibration information is to be recorded in ink in table form using a format similar to that shown in 4.1.2.

The calibration check on deck prior to diving will, in most cases, prevent wasted diving time due to

malfunction of equipment.

Calibrations readings on zinc and magnesium test blocks should read –1.00v to  –1.5 v and –1.45v to –1.50v respectively with reference to the silver / silver half cell.

Should the calibration readings obtained be outside these ranges by +/- 0.05v or more the meter is to be considered non-operational and is to be repaired or replaced.

If the pre-dive and pre-inspection calibration readings obtained were acceptable but the post-

inspection ones are not, all readings taken during the dive are to be retaken using another meter.

Note:

It is important to allow a suitable settling down period prior to use of a cathodic potential measuring instrument. For his reason the meter to be used shall be soaked in salt water, with its tip point upwards, for at least 30 minutes prior to the dive to allow water to displace all air from around the half cell and fully activate the reference system.

    - TESTING REQUIREMENTS

- Prior to diving ensure that the meter in use has been fully charged and has had its calibration checked.

- The contractor shall perform all charging or changing of batteries in a timely manner so as to ensure that the inspection program is not interrupted.

- The measurement location shall be cleaned to bare shiny metal before the reading is taken; the cleaned area shall be the minimum necessary to provide a good contact.

- The minimum acceptable level of protection for a cathodically protected structure in seawater is  -800mv (0.8v) and the client should be informed immediately of any readings which are less negative than –840mv.

In such instances additional readings shall be taken radiating outward along all members adjacent to the low reading until such a point that readings are consistently above -840mv are obtained. In this manner a potential gradient shall be plotted against accurately recorded measurement locations.

  - DETAILED WELD INSPECTION – GENERAL TECHNIQUES

    - DATUM MARKING AND REFERENCE LABELS

The following pages detail the preferred datum locations for each type of weld likely to be encountered. Where these locations prove to be impractical, the datum location is to be selected by the N.D.T. diver carrying out the inspection and to be relayed immediately to the onboard Inspection Engineer.

This section also details the required direction in which the N.D.T. diver is to carry out the inspection of each of the various weld types and in all instances the procedures listed to be adhered to.

Wherever possible for each type of weld likely to be encountered the location at which the datum marks are to be placed should be standardised as follows:

      - GIRTH & SEAM WELDS

- Girth (Butt) Welds in vertical members

Mark the datum points on the North side of the member (including legs) and inspect the weld in a clockwise direction looking up. Refer to figure 4.1

- Girth (Butt) Welds in vertical diagonal members

Mark the datum point at 12 o’clock and inspect the weld in a clockwise direction looking towards the nearest node. Refer to figure 4.1

- Girth (Butt) Welds in horizontal members

This group includes butt welds on both horizontal and horizontal diagonal braces. Datum point to be placed at 12 o’clock, inspect weld clockwise looking towards the nearest node. Refer to figure 4.2

- Seam Welds In Vertical members

Includes seam welds in vertical diagonal members, as well as legs. Mark datum at the upper end of the weld, which is to be inspected from the top downwards. Refer to figure 4.3

- Horizontal Seam Welds

Location of datum to be at either end at the discretion of the diver inspector

      - NODAL WELDS

i)	Brace to leg nodes

Datum marks to be placed as near as possible to the 12 o’clock position and the weld to be inspected in a clockwise direction as viewed form the brace towards the leg. If part of the weld is inaccessible as a result of overlap by another brace, the datum mark should be placed at the first accessible location clockwise of the inaccessible are. Figure 4.4 illustrates this point.

- Brace to Brace Nodes

Datum mark is to be placed at 12 o’clock where possible, otherwise datum should be placed facing the inside of the structure.

Where neither of these actions are practical the datum location is to be selected by the N.D.T. diver carrying out the inspection and relayed to the onboard Inspection Engineer.

In those instances where part of the weld being inspected is inaccessible as a result of overlap by another brace, the procedure outlined above is to be followed.

Refer to the following pages for details of several brace to leg and brace to brace node configurations and the requirements for the inspection of each. Note that in all cases the weld is to be inspected in a clockwise direction facing towards the chord.

Page 4-11

Page 4-12

Page 4-13

Page 4-14

Page 4-15

Page 4-16

Page 4-17

Page 4-18

Page 4-19

Page 4-20

    - WELD DEFECT TERMINOLOGY

The inspection, reporting and remedial action requirements differ for each of the various anomalies/defects likely to be encountered during the inspection of the weld. The following sections describe all of the more common anomalies/defects and detail the inspection and reporting requirements for each:

- Tooling Marks

Marks in the steel surface which are the result of the manufacturing process e.g. chipping marks, grinding marks, punch marks.

Information Required

Location and type only where they are more than 2mm in depth. Tooling marks that penetrate the parent metal further than 2mmnare to be treated as defects and full dimensions are to be recorded.

- Spatter

Globules of weld metal or filler expelled during the welding process and adhering to the surface of the parent metal or solidified weld metal.

Picture of spatter

Information Required   Location only.

- Scar areas

Remnants of sea fastenings, lugs, temporary braces, padeyes etc. burnt off the parent metal.

Picture of scar area

Information Required

Location only, if remnants are proud of parent metal. Any areas where gouging occurs are to be treated as defects and full dimensions, including length, width and depth of intrusion are to be obtained

Action Required

All rough sharp edges within areas of gouging are stress raisers and as such should be ground smooth.

iv)	Weld Writing

This refers to any letter, number, or symbol which has been deliberately ‘written’ on the parent metal with weld material. Typical examples of weld writing may include the welders initials, identification numbers, or similar.

Information Required

Location and approximate size of the letter number or symbol. Such areas of weld deposit are stress raisers, hence, the weld writing and adjacent area is to be visually inspected for signs of associated cracking. Any cracking found is to be treated in accordance with section 4.4.9.

v)	Undercut

The burning away of the parent metal during welding, resulting in a groove at the toe(s) of the weld. May be continuous or intermittent.

Pictures of Undercut

Information Required		Location, length, and if severe, width and depth.

vi)	Cap Concavity:		Concave cap profile’

Pictures of cap concavity

Information Required		Location only

vii)	Incomplete Filled Groove

Otherwise known as insufficient reinforcement. A long continuous or intermittent channel in the surface of a weld due to insufficient deposit of weld metal.

Pictures of Incompletely filled groove

Information Required		Location only

viii)	Lack of Sidewall Fusion

Lack of fusion between the toe of the weld metal and the parent metal. This is potentially serious planner defect that may be more readily detected by M.P.I. than visual inspection.

Picture of lack of side wall fusion

Information Required		Location and full dimensions, length and if possible width and depth.

Action required		defect to be blended (ground out) to maximum depth of

2.5mm into parent metal

- Lack of Inter-run Fusion

Lack of fusion between two different runs of the weld metal.

Picture of lack of inter-run fusion

Information Required		Location and full dimensions, length and if possible width and depth.

Action required		defect to be blended (ground out) to maximum depth of

2.5mm into parent metal

- Lapping (Cold lap, Overlap)

Excess of weld metal at the toe of the weld covering the parent metal surface but not fused to it.

Picture of lack of lapping

Information Required		Location and length.

- Arc strike/Burn

Local damage to the surface of the parent metal resulting from accidental arcing or striking the arc outside the weld groove.

Information Required Location and length. If more than 1.5mm deep into parent metal, also width and depth.

- Pitting

Localised metal attack caused when an area on the metal begins to act as an anode. The anodic area starts to corrode, whilst the surrounding area acts as a cathode and does not corrode.

Information Required   Location deeper than 1.5mm to be measured by pit-gauge. Diameter not required. Areas of excessive pitting to be photographed. Pitting on weld cap to be termed “Preferential Corrosion”.

- Porosity

A cavity in the weld metal caused by entrapped gas. May be grouped or uniformly distributed through the weld metal.

Information Required   Location, diameter and frequency.

- Seam Discontinuities

Linear flaws in the parent metal resulting from incomplete seam fusion during the manufacturing/rolling process and appearing as longitudinal lines along the member.

Information Required   Location and length only.

Action Required	All such discontinuities are to be ground out in 0.5mm steps to a maximum depth of 2.5mm. After each 0.5mm step re-inspect the anomaly and determine whether or not it runs deeper into the wall thickness or is only superficial.

If the discontinuity is still present after 2.5 mm grinding, clean outwards, along the member, to accretion the full length of the flaw and take close-up photographs of it.

- Cracks

A linear discontinuity produced by fracture. Cracks may be longitudinal (parallel to central axis of the weld), transverse (perpendicular to central axis of weld), oblique, edge or crater and may be found in the weld metal toe, fusion zone, underbead, heat affected zone (HAZ) or parent metal.

Cracks are usually formed due to stress.

Although serious cracking may be detected during a visual inspection, it is more usually detected by M.P.I.

The different types of cracks, which may be encountered, are shown below and reference should be made to the next page for a description of the cracks illustrated.

- Transverse crack in the weld metal.

- Group of disconnected cracks, may be situated in the weld metal, heat affected zone or parent metal.

- Longitudinal crack in the weld metal obliquely crossing the axis of the weld. Such cracks may also be found propagating from the toe of the weld into the H.A.Z. The angle is to be measured as well as the usual dimensions.

- Transverse crack in the parent metal propagating from the toe of the weld.

- Longitudinal crack in the H.A.Z. or parent metal.

- Longitudinal branching crack. May be situated in the weld metal, H.A.Z. or parent metal.

- Crater Crack:  a crack that may be longitudinal, transverse or star shaped, located in the end crater of a weld.

- Intermittent longitudinal crack:  May be situated in the parent metal.

- Radiating cracks:  Cracks radiating from a common point, may be found in the weld metal, parent metal or H.A.Z.

Note:	Small cracks of this type are termed as star cracks.

- Toe crack:  A crack situated in the toe of the weld.

- Fusion line cracks, not usually detected by M.P.I.

- Root crack.

- Transverse crack in the parent metal.

Information Required	Location and full dimensions. Where a crack is orientated obliquely to the central axis of the weld the angle is to be determined as in example (3).

Action Required	All cracks are to be ground out, in0.5 mm stages, until they disappear or a maximum of 2.5 mm of weld or parent metal has been removed.

Refer to section 4.4.9 for the grinding procedure to be used.